General Information “Cavity closer”
Solid John Film Faced Plywood ROOF 15mm

Material: Solid John Film Faced Plywood

- Suitable for use class 3

- Composition

  - Wood type: durability class 2 according to EN 636

  - Bonding: class 3 WBP – weather and boil proof according to EN 314

- Weight per m³: 550-650 kg

- Dimensions:

  - 15 mm thick

  - Panel size 1.22 m x 2.44 m

Technical data

- Basis: structural plywood

- Dimensions: 122 * 244 cm

- Thickness: 15 mm

- Reference standard: Use class 3 (EN 636-3)

- Density: 550 - 650 kg/m² (EN 323)

- Average moisture content: 10.2 (EN 322)

- Flexural strength: F60 (EN 636)

- Elasticity: E100 (EN 636)

- Formaldehyde emissions: E1 (EN 13986 - Annex B)

- Reaction to fire: D-s2, d0 (EN 13986 - Annex B)

- Bond class: Class 3 (WBP) (EN 314-1)

- Wood durability class: Class 2 (EN 350)

Installation

- Provide 2 mm joint between 2 different strips.

- Installation based on European standards.

Application

- Closing the cavity wall to create a quality base for the eaves.